## Slide 1: Status of the SPL cavities at CERN
Aviles & N. Valverde
on behalf of SPL team

## Slide 2: Overview
Overview
Copper cavity
Niobium cavity
Tooling
Conclusions

## Slide 3: Overview
Cavity
Helium tank
Inter-cavity
support
Thermal shield
Vacuum vessel
RF coupler
Thermal shield tie-rod
Cold-to-warm
transition
Magnetic shielding
Insulation vacuum
relief plate
Cryogenic circuit
burst disk
Gate valve
Two-phase pipe
Cavity tuner
Double-walled
tube
He phase separator
Cryogenic lines port
Thanks to R. Bonomi and V. Parma

## Slide 4: Overview
Bulk Niobium 5Cells cavity
Stainless steel (316L /316LN) helium tank designed by CERN, supplied by CEA and welded to the cavity at CERN.
Design already validated by CERN.
4 niobium cavities under fabrication at RI – delivery beginning 2013
Tuners provided by CEA. Under testing at CERN
Pumping line & Magnetic shield to be provided IPN Orsay.

## Slide 5: Cooper cavity
Two copper cavities fabricated in order to:
Learn during the fabrication process
RF measurements
Bead pull measurement
Validation of the tooling for the niobium cavity
Surface treatments

## Slide 6: Copper cavity
Cell-by-cell tuning system with RF bead-pull measurements
Mechanical measurements: frequency shift with respect to stress and deformation
Measured cavity frequency change vs. mechanical deformation of cell no 4.

## Slide 7: Copper cavity
Chart: Deformation in fonction of the frequency
| -1.9000000000000001E-4 | -0.49790000000000001 | -0.99750000000000005 | -1.5089999999999999 | -2.0270000000000001 | -2.5219999999999998 | -3.0049999999999999 | -3.22 | 0.1033 | 1.101 | 2.1120000000000001 | 3.0939999999999999 | 3.8780000000000001
 | 0 | -0.0428 | -0.1104 | -0.1731 | -0.2347 | -0.2954 | -0.3533 | -0.3785 | 0.0002 | 0.0413 | 0.1454 | 0.2321 | 0.3036
Cavity tuner: measurement of cavity detuning versus mechanical deformation.

## Slide 8: Reparation monocell from RI at CERN
Machining (preparation before brazing)
Brazing between niobium tube and Stainless steel (316LN) flange.
The monocell has being repaired in order to continue with the electropolishing and cold tests

## Slide 9: Reparation monocell from RI at CERN
EB Welding from the outside (W#1) and inside (W#2)
Full penetration: 2.4 mm
EB Welding from the outside (W#3)
Full penetration: 1.7 mm
Cross section of the EB weld (W#1 +W#2)
Cross section of the EB weld (W#3)

## Slide 10: Niobium cavity at RI
4 niobium cavities fabricated by Research Instruments (RI) will arrive to CERN this year.
1 already at CERN
3 cavities will be delivered middle of December

## Slide 11: Niobium cavity at CERN
Spinning of half-cells and beam tubes at HEGGLI
Dimensional control by CMM
RF measurements.

## Slide 12: Niobium cavity at CERN
Spinning
Machining
Cutting cell length
RF measurement
CP (chemical polishing)
Spinning
Machining – Welding preparation (Iris & rings)
CP
Nb
HALF-CELLS
RF measurements
Assembly half-cell+ half-cell+ stiffening ring=> Dumb-bell
Degreasing + CP (8 h before EBW)
EBW half-cell + half-cell
Degreasing +CP (8 hours before EBW)
EBW dumb-bell+ stiffening ring
RF measurements
Trimming equators
RF measurements
Grinding and CP (if needed)
DUMB-BELLS
EBW
EBW
CP
EBW
Trimming equators
Grinding and CP (if needed)
EBW
Degreasing +CP
Nb
Spinning
Necking-out
Machining
CP
Spinning
Necking-out
Machining
CP
BEAM TUBES

## Slide 13: Niobium cavity at CERN
Nb
Machining SS Flange + Nb beam tube + SS insert
Degreasing + CP
Brazing
Machining-Removal of SS insert
Machining
Brazing
SS
TANK CONNECTOR
EBW
2
Assembly beam tube + ports=> end group
Degreasing + CP ( 8h before EBW)
Electron beam welding (EBW)
CP
END GROUP
Machining SS Flange + Nb tube + SS insert
Degreasing + CP
Brazing
Machining- Removal of SS insert
Brazing
Machining
Nb
SS
FLANGES
SS
Degreasing
BEAM FLANGES
Machining SS Flange + Nb beam tube + SS insert
Degreasing + CP
Brazing
Machining-Removal of SS insert
Brazing
Machining
SS
Degreasing
SS
Nb
SS

## Slide 14: Niobium cavity at CERN
RF measurements
Trimming
EBW
EBW
RF measurements
EXTREMITY 1
EBW
CP
Cp
Assembly end group+ tank connector + half-cell=> extremity 1
Degreasing + CP ( 8h before EBW)
EBW end group + tank connector
Degreasing + CP ( 8h before EBW)
EBW end group + half-cell
RF measurements
Trimming equator
RF measurements
Assembly end group + half-cell=> extremity 2
Degreasing + CP ( 8h before EBW)
EBW end group + half-cell
RF measurements
Trimming equator
RF measurements
EBW
Trimming
RF measurements
RF measurements
EXTREMITY 2
CP

## Slide 15: Niobium cavity at CERN
Final assembly
CP - 8 h before each EBW
EB Tack weld
EBW
EB Tack weld
EB Tack weld
EB Tack weld
EBW
EBW
EBW

## Slide 16: Ancillaries
5 stainless steel helium tanks (designed by CERN) will be delivered by CEA in January

## Slide 17: Ancillaries
Electron beam welding tooling designed and fabricated at CERN

## Slide 18: Ancillaries
Tooling for electropolishing
Tooling for cold tests
Tooling already fabricated and available at CERN

## Slide 19: Conclusions
Copper cavities have proven to be very useful for the different testing campaigns carried out during the last year. The results obtained will be extremely valuable for the tuning operation of the niobium cavities
4 niobium five – cell cavities will be delivered to CERN by the end of the year
A fifth niobium cavity is under fabrication at CERN
5 helium tanks will be supplied by CEA in January 2014

## Slide 20
Thank you very much
QUESTIONS??