## Slide 1: i-CDR committee on welds of port tubes on monolith vessel
Peter rådahl, ESS Chief engineer, chair of the i-CDR
DR. Bertrand Nicquevert, advisor to the ESS technical director, secretary of the i-CDR
On behalf of the whole committee
Questions and answers

## Slide 2: Q&A 1
Welding sequence
a) What is the proposed order of the sequence for tack weld, if already defined?
b) The estimation of the induced deformations of the vessel is rather wide and global so far. Any chance to get a better estimate of the level of these deformations at which positions, and hence a better guess of the corresponding shape after weld?
c) Was the add-up of a (removable or not) stiffener ring considered?
d) Was the chance of the PT sticking (instead of sliding) along x, for instance due to restrain devices in y or z, estimated?

## Slide 3: Q&A 2
Tolerance budget
a) Given the sensitivity of the vessel, which new deformations may have to be considered when going from (possibly cold) room temperature to operation temperature? Can this lead to, for instance, a move in z of the port tube welded face, and consequently of a rotation of the whole PT around y? What about shear in the weld if this move would be prevented? Any chance to measure residual stress before / after?
b) What are the remaining opportunities to increase the adjustability of NBOAs in the port tubes in y and z?
c) Influence of a non-uniform gap after welding: due to the lever arm of 2.7m, in order to eat up the 1mm budget, this is enough to get an unbalanced thicknes of left vs right sides of less than 0.1 mm. It is appreciated that this move would be prevented by y-restraining-devices. What is the corresponding induced load? Were the restraining devices dimensioned to take up this load? Was the induced residual stress in the weld estimated?

## Slide 4: Q&A 3
Welding Tests, global tests, risk analysis
A) Welding tests:
- what are the VT plans, and were the respective advantages of dye penetrant wrt to enhanced VT (lens or fiberscope) considered?
- what are the technical issues preventing applying UT in complement of RT?
B) pressure / vacuum /leak tests:
- to which extent are those tests considered as acceptance criteria for the ENSA contract? for the ESS Bilbao contribution?
C) risk analysis
- has ESS Bilbao prepared a risk analysis complementing ENSA’s one for the remaining risk factors?