## Slide 1
Towards very cold neutrons
Oliver Zimmer
LENS moderator meeting; Garching, 24 March 2023

## Slide 2
Contents:
Why very cold neutrons (VCN)?
Moderation to the VCN range - local excitations
Clathrate hydrates as VCN moderator and CN reflector
HighNESS: studies of moderator material properties
Collaboration on VCN moderator prototype with ILL?

## Slide 3
Why Very Cold Neutrons?
Neutron scattering community:
Particle physics community:
  Sensitivity improvements:
    neutron-antineutron oscillation experiment ( 2)
    in-beam neutron EDM experiments ( )
From proceedings of workshop on application of a VCN source at Argonne, 2005
Revisited during recent ESS workshop on CN, VCN and UCN sources

## Slide 4
How to get cool neutrons?
 |  (Å) | Tn (K)
thermal | 1.8 | 300
cold | 5 | 30-100
very cold | > 15 | < 4
ultra cold | > 500 | “0.002”
Moderation:
slowdown with many inelastic interactions
 thermal equilibrium with cold medium
needs weakly absorbing cold medium with
good scattering cross sections
Moderation: compression
of full neutron spectrum

## Slide 5
thermal  cold:
liquid H2 and D2 cold sources
(quasi-elastic scattering)
solid methane
(molecular rotations)
thermal/cold  very cold?
phonons ?
kinematic restriction due to dispersion
T < TD & E < kBTD : 1-phonon-emission  E -3
Gurevich and Tarasov,
Slow Neutrons
 |  (Å) | Tn (K)
thermal | 1.8 | 300
cold | 5 | 30-100
very cold | > 15 | < 4
ultra cold | > 500 | “0.002”

## Slide 6
better use incoherent scattering by local modes:
(1) molecular rotations
(2) librational (Einstein) modes of confined molecules

## Slide 7
O2 is paramagnetic and has a triplet zero-field splitting
!
Em
… no magnetic field needed !
m = 0
m = 1
better use incoherent scattering by local modes:
(1) molecular rotations
(2) librational (Einstein) modes of confined molecules
(3) weakly absorbing paramagnetic species:

## Slide 8
Neutron slowdown in medium at kBT < E *,
(E *  4.6 K for zero-field splitting in molecular O2)
see Phys. Rev. C 93, 035503 (2016) for analysis of slowdown in infinite medium
Einstein modes can short-circuit a long paramagnetic cascade

## Slide 9
Solid oxygen is antiferromagnetic at low T (dispersion and dangerous), but:
Clathrate hydrate with O2 as guest molecule:
O2 density (90 % cage filling)
stays paramagnetic at liquid-He temperatures
metastable (non-explosive)
neutron lifetime if fully deuterated
Methane hydrate clathrate

## Slide 10
Clathrate hydrates
 | Clathrate type I | Clathrate type II
structure | cubic, a = 12 Å | fcc, a = 17.1 Å
# H2O per unit cell | 46 | 136
Cages per unit cell | 6 large + 2 small | 8 large + 16 small
Bragg cut-off wavelength | 24 Å | 20 Å
Guest molecules, e.g., | CH4 | O2 , C4H8O (THF)
Large choice of weakly absorbing molecules made of D, O and C
non-dangerous materials
Gas hydrates meta-stable up to 140 K (O2, CH4); not so easy to produce
THF-d clathrate stable up to 70 Celsius; very easy to produce
Huge lattice constants  large Bragg cut-off  albedo in whole CN -range
THF
CH4
Exemplary
guests:

## Slide 11
Tetrahydrofuran (THF) clathrate hydrate
 | Clathrate type I | Clathrate type II
structure | cubic, a = 12 Å | fcc, a = 17.1 Å
# H2O per unit cell | 46 | 136
Cages per unit cell | 6 large + 2 small | 8 large + 16 small
Bragg cut-off wavelength | 24 Å | 20 Å
Guest molecules, e.g., | CH4 | O2 , C4H8O (THF)
Neutron scattering measurements done at ILL in 2021 and 2022 on:
  17D20:THF-d 17H20:THF-d 17D20:THF 17H20:THF
main goal within WP3 of HighNESS: S(q,) in absolute units
Stoichiometric compound: 17H20:THF
Can be annealed by re-melting and re-freezing
(forms polycrystalline clathrate structure)
THF

## Slide 12
Tetrahydrofuran (THF) clathrate hydrate
Neutron scattering measurements done in 2021 and 2022 on:
  17D20:THF-d 17H20:THF-d 17D20:THF 17H20:THF
main goal within WP3 of HighNESS: S(q,) in absolute units
exemplary IN5 data:
Richard Wagner (HighNESS postdoc)
Valentin Czamler (HighNESS PhD stud.)

## Slide 13
THF + O2 binary clathrate hydrate
 | Clathrate type I | Clathrate type II
structure | cubic, a = 12 Å | fcc, a = 17.1 Å
# H2O per unit cell | 46 | 136
Cages per unit cell | 6 large + 2 small | 8 large + 16 small
Bragg cut-off wavelength | 24 Å | 20 Å
Guest molecules, e.g., | CH4 | O2 , C4H8O (THF)
Combines strong motional modes of THF-d with paramagnetic cooling by O2
Should improve moderation w.r.t. the simple 17D20:THF-d
+ : simpler to prepare than a pure gas hydrate, but:
– : cannot be simply annealed  likely applicable only for weaker sources
O2
THF

## Slide 14
Magnetic intensity seems in agreement with theoretical prediction
First experiments on O2 clathrate done at D20, IN4, IN6 and D7
(exp. Team: A. Falenty, T. Hansen, M. Koza, W. Kuhs, OZ)

## Slide 15
Possibility at ILL: PF1B cold neutron beam facility
(instrument scientists: Torsten Soldner & Valery Nesvizhevsky)

## Slide 16
Invitation for collaboration with ILL
Common grant application?
As a next step after HighNESS:
Construction and characterization of VCN moderator prototype
30 liters of 17D2O.THF-d, cooled to 1.3 K, cryogenics from EURIZON
Monochromatic beam at PF1B with velocity selector
ToF analysis of moderated neutrons (, Tmod and position)
without/with nanodiamond reflector
Comparison of exp. results with simulations, tests of radiation hardness, other materials, test in neutron field at Budapest reactor? …
Velocity selector
ToF analysis
ToF analysis
ToF analysis
ToF analysis
VCN moderator