## Slide 1
Activation of the ISIS TS-1 and TS-2 targets
- Simulations vs. experimental results -
Goran Škoro*
* On behalf of: S. Ansell, F. Burge, D. Ashcroft, G. Burns, D. Findlay…

## Slide 2
ISIS TARGETS
DATES FITTED - REMOVED
TS1
…
TANTALUM #2 OCT 1994 – FEB 1995
URANIUM #9 MAY 1995 – JUN 1995
TANTALUM #2 JUN 1995 – SEP 1996
TANTALUM #3 NOV 1996 – APR 1999
TANTALUM #4 MAY 1999 – MAR 2001
TUNGSTEN #1 MAY 2001 – AUG 2005
TUNGSTEN #2 SEP 2005 – APR 2009
TUNGSTEN #3 APR 2009 – SEP 2014
TUNGSTEN #4 MAR 2015 –
TS2
TUNGSTEN #1 AUG 2008 – FEB 2010
TUNGSTEN #2 FEB 2010 – JUN 2010
TUNGSTEN #3 MAR 2011 – NOV 2012
TUNGSTEN #4 NOV 2012 – JUN 2014
TUNGSTEN #6 JUL 2014 – JUL 2015
TUNGSTEN #7 SEP 2015 –
TS1
TS2
ISIS Target Stations
BEAM PARAMETERS
800 MeV protons
50 Hz
Short pulse (~0.5 µs)
160 µA – TS1
40 µA – TS2

## Slide 3
Uranium target
TS-1 target(s)
Tungsten target
Tantalum target

## Slide 4
TS-1 TRaM (MCNPX model)
Tungsten target

## Slide 5
800 MeV protons (50 Hz)
TS-1 target activation
Simulations vs. experimental results
- long cooling times -

## Slide 6
Nuclide Halflife,s 0.00E+00 s 1 year 2 years 2.9 years 6.6 years _______ __________ __________ __________ __________ __________ __________ H 3 0.3888E+09 0.1393E+14 0.1316E+14 0.1244E+14 0.1183E+14 0.9773E+13 Na 22 0.8211E+08 0.4344E+11 0.3329E+11 0.2550E+11 0.2006E+11 0.7487E+10 Ar 39 0.8489E+10 0.2270E+10 0.2264E+10 0.2258E+10 0.2253E+10 0.2231E+10 Ca 45 0.1406E+08 0.1947E+12 0.4106E+11 0.8660E+10 0.2134E+10 0.6737E+07 Sc 44 0.1414E+05 0.3260E+13 0.1382E+11 0.1362E+11 0.1344E+11 0.1273E+11 Sc 46 0.7240E+07 0.4278E+13 0.2085E+12 0.1016E+11 0.6697E+09 0.9350E+04 Ti 44 0.1493E+10 0.1403E+11 0.1382E+11 0.1362E+11 0.1344E+11 0.1273E+11 V 49 0.2920E+08 0.7943E+13 0.3756E+13 0.1776E+13 0.9050E+12 0.5663E+11 Mn 54 0.2697E+08 0.2640E+14 0.1173E+14 0.5213E+13 0.2512E+13 0.1249E+12 Fe 55 0.8615E+08 0.6199E+14 0.4809E+14 0.3731E+14 0.2968E+14 0.1160E+14 Co 57 0.2348E+08 0.1019E+14 0.4025E+13 0.1586E+13 0.6857E+12 0.2185E+11 Co 58 0.6127E+07 0.2679E+14 0.7579E+12 0.2134E+11 0.8586E+09 0.1575E+04 Co 60 0.1664E+09 0.3142E+12 0.2755E+12 0.2416E+12 0.2146E+12 0.1319E+12 Ni 59 0.2367E+13 0.5318E+10 0.5318E+10 0.5318E+10 0.5318E+10 0.5317E+10 Ni 63 0.3159E+10 0.6269E+12 0.6229E+12 0.6185E+12 0.6146E+12 0.5991E+12 Ba133 0.3320E+09 0.8378E+11 0.7844E+11 0.7343E+11 0.6920E+11 0.5423E+11 Ce139 0.1189E+08 0.3759E+13 0.5974E+12 0.9493E+11 0.1814E+11 0.2009E+08 Pm143 0.2290E+08 0.5254E+13 0.2021E+13 0.7777E+12 0.3292E+12 0.9608E+10 Pm144 0.3140E+08 0.4744E+10 0.2364E+10 0.1178E+10 0.6293E+09 0.4780E+08 Pm145 0.5586E+09 0.5257E+12 0.7705E+12 0.8668E+12 0.8926E+12 0.8226E+12 Pm146 0.1745E+09 0.4507E+10 0.3976E+10 0.3508E+10 0.3134E+10 0.1971E+10 Sm145 0.2938E+08 0.9499E+13 0.4662E+13 0.2214E+13 0.1133E+13 0.7206E+11 Eu149 0.8040E+07 0.1386E+14 0.1050E+13 0.6914E+11 0.5976E+10 0.2539E+06 Eu150 0.1130E+10 0.1150E+10 0.1128E+10 0.1106E+10 0.1087E+10 0.1012E+10 Eu152 0.4206E+09 0.3977E+11 0.3776E+11 0.3584E+11 0.3421E+11 0.2822E+11 Eu154 0.2711E+09 0.1037E+11 0.9566E+10 0.8825E+10 0.8208E+10 0.6089E+10 Gd148 0.2354E+10 0.3080E+12 0.3051E+12 0.3023E+12 0.2998E+12 0.2897E+12 Gd151 0.1071E+08 0.1364E+14 0.1784E+13 0.2315E+12 0.3683E+11 0.1925E+08 Gd153 0.2087E+08 0.9389E+13 0.3348E+13 0.1174E+13 0.4573E+12 0.9470E+10 Tb157 0.4734E+10 0.2407E+12 0.2396E+12 0.2385E+12 0.2375E+12 0.2335E+12 Tb158 0.4734E+10 0.4398E+10 0.4377E+10 0.4357E+10 0.4339E+10 0.4265E+10 Dy159 0.1248E+08 0.1675E+14 0.2902E+13 0.5026E+12 0.1037E+12 0.1580E+09 Ho163 0.1442E+12 0.7770E+10 0.7769E+10 0.7767E+10 0.7766E+10 0.7762E+10 Tm170 0.1111E+08 0.4034E+12 0.5633E+11 0.7866E+10 0.1337E+10 0.9181E+06 Lu172 0.5790E+06 0.3379E+14 0.1621E+14 0.1119E+14 0.8015E+13 0.2033E+13 Lu173 0.4320E+08 0.3548E+14 0.2147E+14 0.1294E+14 0.8205E+13 0.1261E+13 Lu174 0.1045E+09 0.2037E+13 0.1664E+13 0.1352E+13 0.1120E+13 0.5164E+12 Lu174* 0.1227E+08 0.1430E+12 0.2404E+11 0.4044E+10 0.8130E+09 0.1110E+07 Hf172 0.5900E+08 0.2326E+14 0.1605E+14 0.1108E+14 0.7937E+13 0.2013E+13 Hf175 0.6048E+07 0.4209E+14 0.1145E+13 0.3075E+11 0.1187E+10 0.1831E+04 Ta179 0.5745E+08 0.1682E+15 0.1150E+15 0.7855E+14 0.5576E+14 0.1363E+14 Ta182 0.9887E+07 0.8883E+16 0.9721E+15 0.1064E+15 0.1452E+14 0.4047E+10 W 181 0.1047E+08 0.2366E+15 0.2932E+14 0.3630E+13 0.5540E+12 0.2439E+09 W 185 0.6489E+07 0.6758E+15 0.2322E+14 0.7976E+12 0.3838E+11 0.1470E+06
TS1 tungsten target inventory
TS1 W2
TS1 W1
* - Expected large contribution to the gamma dose rate
MCNPX/CINDER90
CEM03
Total: 2676 mAhrs
TS1-W1
TS-1 target(s) activation: initial calculation done in 2012
Detailed model of the TS-1 did not exist (details of the TS-1 TRaM geometry just started to be collected). Activation calculation was required for a new license for disposal of the first tungsten target so it was important not to underestimate the target activity.
Target geometry - very detailed model; surrounding area geometry – not really (just the reflector – no moderators, flightlines, decouplers, pipes, etc…)

## Slide 7
Gamma spectrometry
- Target in the flask -
4 cm Pb
~17 cm Pb
hottest spot
March 2012

## Slide 8
TS-1 targets:
Gamma spectrometry
TS-1 W1
2676 mAhrs
6.6 years cooling
Co-60; Lu-172

## Slide 9
TS-1 targets:
Gamma spectrometry
TS-1 W2
1947 mAhrs
2.9 years cooling
Co-60; Lu-172;
+ Ta-182

## Slide 10
800 MeV protons (50 Hz)
Comparison between old (2012) and new (2017) results
A few comments
Tungsten: “practically” no change;
Tantalum: 30% drop at the end of irradiation; small drop for very long cooling times;
Steel: factor of 2 drop for all cooling times;
Total activity
The effect (total activity reduction) is decreasing when going from outside to the centreline of the target: reflected neutrons contribution is reduced in new calculations!
Conclusion
Previous calculation has overestimated the total activity (particularly at short cooling times).
TS-1 target(s) activation: new calculation done in 2017
Very detailed model of complete TS-1 TRaM (part of the latest TS-1 neutronics model);
Target cooling water is a mixture: 80% D2O - 20% H2O (pure D2O in previous calculations)…

## Slide 11
Gamma spectrometry – new measurements
TS-1 W2 target; 1946 mA-hours in fifteen irradiation ‘campaigns’ each ~30–50 days long; cooling time = 7.63 years – to coincide with the date on which the gamma-ray spectroscopy measurements were made.
same idea…

## Slide 12
800 MeV protons (50 Hz)
TS-1 target activation
Simulations vs. experimental results
- short cooling times -

## Slide 13
800 MeV protons (50 Hz)
TS-1 W4 target
Decay power and temperature measurement
30. 11. 2016.
Temperature [°C]

## Slide 14
800 MeV protons (50 Hz)
Beam Status | Number of days | Integrated current [mA-hours] | Beam energy [MeV]
on | 47 | 171 | 700
off | 30 |  | 
on | 42 | 162 | 700
off | 44 |  | 
on | 38 | 139 | 700
off | 16 |  | 
on | 43 | 142 | 800
off | 61 |  | 
on | 16 | 53 | 800
on | 22 | 72 | 700
off | 17 |  | 
on | 38 | 138 | 800
off | 112 |  | 
on | 15 | 41 | 800
on | 30 | 83 | 700
off | 17 |  | 
on | 16 | 39 | 700
TS-1 W4 target:
irradiation history
Cycle: 2014/03
Cycle: 2016/04
up to 30-Nov-2016
For short cooling times, (average) current in the last cycle is very important (equally important as total integrated current over the target life).

## Slide 15
TS-1 W-4 target decay power
For short cooling times, (average) current in the last cycle is very important (equally important as total integrated current over the target life). In this case, during first 2 weeks of 2016/04 cycle, average current was pretty low (102 µA).
Decay power on 30 November 2016 (when the beam was switched off ) is ~ 1 kW.
MCNPX/CINDER90 calculations

## Slide 16
Rate of the temperature rise – simulation vs. measurement
Distribution of decay power along
the target (30 November 2016)
MCNPX/CINDER90 calculations
* D. J. S. Findlay, private communication, 2017.
*
*

## Slide 17
800 MeV protons (50 Hz)
Appendix
TS-2 target

## Slide 18
TS-2 target
Current target – tungsten cylinder (tantalum cladding)
Typically 40 µA (800 MeV protons)
  Solid methane
  Liquid hydrogen
  Solid Be

## Slide 19
Gamma spectrum of TS2 cooling system filter – 10 days after beam off
182Ta
1121 keV; 35%
1222 keV; 26%
1189 keV; 16%
1231 keV; 11%
1093 keV; 62%
901 keV; 30%
912 keV; 15%
810 keV; 17%
172Lu
November 2012

## Slide 20
Tungsten
Tantalum
Water
Water
Water
* Irradiation = 215.7 mA-hours; cooling time = 10 days
1/4
5/7
1/2000
1/400
1/200
A(172Lu)/A(182Ta)
Ratio of 172Lu and 182Ta activity in different regions of TS-2 W3 target (MCNPX/CINDER90 calculations*)
Conclusion:
Strong indication that radioactive material in the TS2 water cooling system is predominantly Tungsten.

## Slide 21
Direct confirmation: 187W – next cycle, and one after that, and one after that, ..
187W: T1/2 = 1 day