## Slide 1: Accelerator Technologies SRF Proton Accelerator
Christine Darve
Nordic Particle Accelerator School, NPAS2017
https://npap.eu/
Lund University
August 18, 2017

## Slide 2: References
US-Particle Accelerator School, http://uspas.fnal.gov/materials/materials-table.shtml
CERN Accelerator School, http://cas.web.cern.ch/cas
JUAS, https://espace.cern.ch/juas/SitePages/Home.aspx
Few books
RF Linear Accelerators, T.P. Wangler, Wiley, 2008
RF Superconductivity for Accelerator, H. Padamsee, J. Knobloch, T. Hays, Wiley, 2011
An introduction to particle accelerators, E.J.N. Wilson, Oxford Univ. Press, 2001
An introduction to the physics of high-energy accelerators, D.A. Edwards & M.J. Syphers, Wiley, 1993
Project example: ESS SRF Linac Collaborative Space: https://confluence.esss.lu.se/display/CRYOM
ESS SRF Collaborations:

## Slide 3: Outline
  Accelerator ingredient
  Accelerator Environment: Superfluidity and Superconductivity
  Application to Cavity:
    Cavity model
    SRF cavity fabrication
    Cryomodules function
    Cavity package
    Cryomodules
  Application to Magnet: cryo-magnets at LHC
Notes: Zoom in ( previous talk on magnets and cavity)

## Slide 4: Proton Accelerator Main Ingrédients
    1- Ion Source to produce the charged particles to be accelerated
    4- Vacuum chamber to minimize scattering of the beam particles by gas particles – see Pauli’s talk
    3- Magnets are used to bend and focus the particle trajectories –
    see Sverker and Franz’s talks
    2- Accelerating structures to accelerate charged particles –
    see Anders &Mamad’s talks
    5- Cooling systems to remove the heat dissipated in accelerator components; use of superconducting magnet and cavity – see this talk
    6- Beam diagnostics to provide information about the beam intensity (current), position, beam profile and beam loss – see Maja’s talk
    7- Control system to record and control each equipment – see this talk

## Slide 5: Example of Linear Accelerator design
Chart: Beam Beta
[SRF2013 – “The ESS Superconducting Linear Accelerator”, C. Darve, M. Eshraqi, M. Lindroos, D. McGinnis, S. Molloy, P. Bosland and S. Bousson]
Spokes
Medium β
High β
DTL
MEBT
RFQ
LEBT
Source
HEBT & Contingency
Target
2.4 m
4.6 m
3.8 m
39 m
56 m
77 m
179 m
75 keV
3.6 MeV
90 MeV
216 MeV
571 MeV
2000 MeV
352.21 MHz
704.42 MHz
Spoke
M-b
H-b
NC FE
Key parameters:
     5 MW average beam power
    2.86 ms long pulses
    2 GeV
    62.5 mA peak
    14 Hz
    4 % duty cycle
    Protons (H+)
    Minimize and recycle energy use
    Flexible design for mitigation & future upgrades
Style | Spoke | Medium-b | High-b
Frequency (MHz) | 352.21 | 704.42 | 704.42
Number | 26 | 36 | 84
Acc. gradient (MV/m) | 9 | 16.7 | 20
b_geo | 0.5 | 0.67 | 0.86
Velocity range | 0.42 to 0.58 | 0.58 to 0.78 | 0.78 to 0.95
Distance (m) | 56 | 77 | 179
Notes: 312 m SC+ 50 m NC
400 m/ 600 m tunnel = SRF
CO2 neutral..

## Slide 6: A cold technology environment
More than 95 % of the ESS accelerator depends on the success of Superconducting RF (SRF) Cavity technology !!
Cryogenics environment is needed to achieve larger SRF cavity gradients, hence shorter Linac and lower operating cost (effective at long term).
20 tons of “cold mass” to lower to 2 K: i.e. SRF cavities housed in cryomodules
Helium cryoplant capacity: 3 kW at 2 K, 11 kW at 40 K plus liquefaction
LHe and LH2 main risk: expansion of a factor 700 !
Notes: 3kW at 2 K, 10.8 kW at 40 K and 9 g/s
liquefaction capacity for power coupler cooling.
Energy storage – magnet …. Gjoule, LHC example,

## Slide 7: Outline
  Accelerator ingredient
  Accelerator Environment: Superfluidity and Superconductivity
  Application to Cavity:
    Cavity model
    SRF cavity fabrication
    Cryomodules function
    Cavity package
    Cryomodules
  Application to Magnet: cryo-magnets at LHC
Notes: Zoom in ( previous talk on magnets and cavity)

## Slide 8: Why SC cavity and magnet ?
Nb is 105 less (electric) resistant than Cu
@100 MHz, Copper, Rsvs. Nb Rs
    Skin depth :
    AC : Rs==
 @ 2 K, He is 2.103 more (heat) conductive than Cu
 Resistivity of Cu is 1018 higher than for superconductor
Copper at RT: r = = 1.7 10-8 W.m
Superconductor  10﻿−﻿26 Ω. m

## Slide 9: Cooling with Helium
Boiling helium I (normal helium)
  1 W/cm2 in nucleate boiling with 0.5 K temperature rise to the object surface so equivalent to 2 W/cm2K
Forced convection helium I
  Convection coefficients on the order of
  0.1 W/cm2K
Saturated helium II (superfluid helium)
  1 W/cm2 heat transport to the surface without bubbles
Pressurized helium II
  Kapitza conductance about 0.6 W/cm2K
LHC operation
Tevatron operation
 Helium (25 %) is the most common element in Universe after Hydrogen (73 %)
 Two isotopes: 3He (fermion) & 4He (boson)

## Slide 10: Superfluidity Helium- The two-fluid model
Normal-fluid fraction:
excited states atom (phonons & rotons)
 like a conventional viscous fluid
finite density , rn
finite viscosity, 
entropy, s
Macroscopic quantum physic system simplification
The two-fluid model is only a phenomenological model !
Superfluid fraction:
- atoms that have undergone BEC
 like an ideal inviscid liquid resulting in the absence of classical turbulence.
finite density, rs
NO viscosity
carry NO entropy
irrotational behavior for an inviscid fluid
but vortices can be generated in the superfluid component
Quantized vortices
Counter-flow turbulence

## Slide 11: Thermal conductivity of helium II
High flux regime
dT/dx ~ q3
Low flux regime dT/dx ~ q
Heat transport regimes at 1.9 K
Laminar
Turbulent
Mutual- friction regime
No bulk flow
Heat flux
Counter-flow mechanics
e.g. d > 1 mm, q > 10 mW/cm2
In mutual friction regime:
AGM Gorter-Mellink mutual friction parameter
Thermal resistivity function
Internal convection of the super-fluid and normal-fluid components
Notes: D1~ 10 micron for 10-4K/m
Cu (@3.6 K) = 1.2 W/cm2 ; He I (@3.6 K) = 3.6 e-6 W/cm2
Cu (@1.9 K) = 1.6 W/cm2 ; He II (@ 1.9 K) = 24 W/cm2
Heater changes super fluid
into normal. More super
flows through plug
increasing pressure in
container, and fluid squirts
out top in a fountain

## Slide 12: Perfect cooling for Magnets & SRF
Superconducting magnets are often cooled with subcooled liquid
  Typically working near the limit of the superconductor with large stored energy
  Ensure complete liquid coverage and penetration
Superconducting RF cavities are generally cooled with a saturated bath
  Large surface heat transfer in pool boiling for local “hot spots”
  Stable pressures, avoid impact of pressure variation on cavity tune (vs. He I)

## Slide 13: Superconducting magnets

## Slide 14: Superconducting cavities

## Slide 15: Outline
  Accelerator ingredient
  Accelerator Environment: Superfluidity and Superconductivity
  Application to Cavity:
    Cavity model
    SRF cavity fabrication
    Cryomodules function
    Cavity package
    Cryomodules
  Application to Magnet: cryo-magnets at LHC
Notes: Zoom in ( previous talk on magnets and cavity)

## Slide 16: Particle Accelerators need RF Cavity (see Anders’s talk)
ElectroMagnetism – Lorentz and Maxwell
DC
AC
Magnet
Cavity
Electric Field
Magnetic Field
Out
In
Wall Current
(For the fundamental mode at one instant in time)
Notes: ADD 3 FINGERS..

## Slide 17: Recall: RF Cavity shape
Small b
Spoke cavity
Electrical field line of a pi mode
Equivalent circuit for a 4 cell cavity with beam pipe
Spokes
Medium β
High β
DTL
MEBT
RFQ
LEBT
Source
HEBT & Contingency
Target
2.4 m
4.6 m
3.8 m
39 m
56 m
77 m
179 m
75 keV
3.6 MeV
90 MeV
216 MeV
571 MeV
2000 MeV
352.21 MHz
704.42 MHz
High b: Elliptical cavity

## Slide 18: RF Cavity - RLC Model for Cavity Mode
Position:
Amplitude:
Width
Function of geometry and cavity material
Function of geometry
Around each mode frequency, we can describe the cavity as a simple RLC circuit.
Req is inversely proportional to the energy lost
Leq is proportional to the magnetic stored energy
Ceq is proportional to the electric stored energy
Beam
RF Input
Power Amplifier
(Klystrons)
Power Coupler
Gap
Waveguide
EM fields enclosed in a cavity with resonant frequency matching that of RF generator

## Slide 19: RF Cavity RLC Parameters for a Transmission Line Cavity
For the fundamental mode of the transmission line cavity:
The transfer impedance of the cavity is:

## Slide 20: Cavity Quality factor
If the cavity walls are lossless, then the boundary conditions for a given mode can only be satisfied at a single frequency.
The Quality factor is defined as:
Normal conducting  104
Superconducting  1010

## Slide 21: SRF Cavities Performances
Few limitations of performance:
Thermal Breakdown, alias quench
Field Emission: Electron induced by an electrostatic field
Multipacting: secondary electron emission in resonance avalanche
How to limit power loss in the cavity wall ?
By using low-resistant material or superconductors
By rounding the shape to optimize the field distribution
Limit shape edge to prevent field emission
Good vacuum to limit breakdown
Courtesy Ciovati
Notes: Shunt impedance – R/Q = Vˆ2 / wW
W is the maximum energy stored.

## Slide 22: Outline
  Accelerator ingredient
  Accelerator Environment: Superfluidity and Superconductivity
  Application to Cavity:
    Cavity model
    SRF cavity fabrication
    Cryomodules function
    Cavity package
    Cryomodules
  Application to Magnet: cryo-magnets at LHC
Notes: Zoom in ( previous talk on magnets and cavity)

## Slide 23: ESS Requirements and RF Parameters
 | Medium | High
Geometrical beta | 0.67 | 0.86
Frequency (MHz) | 704.42 | 
Number of cells | 6 | 5
Operating temperature (K) | 2 | 
Epk max (MV/m) | 45 | 45
Nominal Accelerating gradient (MV/m) | 16.7 | 19.9
Q0 at nominal gradient | > 5e9 | 
Qext | 7.5 105 | 7.6 105
Iris diameter (mm) | 94 | 120
Cell to cell coupling k (%) | 1.22 | 1.8
p,5p/6 (or 4p/5) mode sep. (MHz) | 0.54 | 1.2
Epk/Eacc | 2.36 | 2.2
Bpk/Eacc (mT/(MV/m)) | 4.79 | 4.3
Maximum. r/Q (W) | 394 | 477
Optimum b | 0.705 | 0.92
G (W) | 196.63 | 241
RF peak power (kW) | 1100 | 
Elliptical cavities
Spoke cavities
Frequency (MHz) | 352,2
Optimum beta | 0,50
Operating temperature (K) | 2
Nominal Accelerating gradient (MV/m) | 9
Lacc (bopt.x nb gaps x l/2) (m) | 0,639
Bpk (mT) | 79 (max)
Epk (MV/m) | 39 (max)
Bpk/Eacc (mT/MV/m) | <8,75
Epk/Eacc | <4,38
Beam tube diameter (mm) | 50
RF peak power (kW) | 335
G (W) | 130
Max R/Q (W) | 427
Qext | 2,85 105
Q0 at nominal gardient | 1,5 109

## Slide 24: Design: ESS High-beta cavity

## Slide 25: Design: SRF Cavities Development
Ti He vessel
Hydroformed Ti bellows
(+/- 3mm range)
Power coupler port
 Stiffeners on the Spoke bars
(vacuum pressure)
Stiffeners (LFD compensation)
Elliptical cavities
Spoke cavity
High beta:
5 cells – beta=0.86
Length 1316,91mm
Medium beta:
6 cells – beta=0.67
Length 1259,40mm
NbTi flange
(w/bore holes for alignment & assembly tool)
+Al hex. gaskets
418 mm
550 mm
994 mm
 No HOM power couplers

## Slide 26: How to fabricate a SRF cavity…
F. Peauger

## Slide 27: Fabrication: Field flatness tooling at CEA
D. Roudier
Exemple of cavity tuning (High beta Prototype n°2 from RI)

## Slide 28: Elliptical Cavity Preparation
Vertical Electropolishing system@ CEA
High-beta cavity fabrication (Zanon and RI)
    Example of the tooling for the assembling of the coupler on the cavity in clean room

## Slide 29: Chemical treatment set-up
F. Eozenou, C. Servouin
Electro-Polishing: EP
Buffer Chemical Polishing: BCP

## Slide 30: Why Surface Polishing ?
    Courtesy Claire Antoine

## Slide 31: Why Surface Polishing ?

## Slide 32: Why do we need clean-room ?
Dust particles and scratches are at the origin of field emission
Courtesy Claire Antoine

## Slide 33: Cavity clean room assembly with High Pressure Rinsing
F. Eozenou, C. Servouin
HPR 100 bars - Ultra pure water
Flanges and antenna pick-up assembly under class 100 laminar flow

## Slide 34: Vertical test results
High beta prototype cavity n°1 from ZANON
Mounting on vertical insert , Connexion to RF system and vacuum pumping station

## Slide 35: Spoke cavity Performances (Jan-June 2015)
Eacc_max=15.3 MV/m achieved with “Romea”
Several MP barriers but easily processed.
Qo > 1.6 1010
Strong FE at max gradient
Limitation is the cooling capacity (unstable conditions, cavity in vertical position)
Spoke cavity exceeding ESS requirements in vertical test on both Eacc and Qo

## Slide 37: Radioprotection improvement for CV tests
Vertical cryostat
Eucard / SPL beta=1 704 MHz cavity
at 19 MV/m, radiation level decreased from 50 to 0.25 µSv/h close to workstation (public limit < 0.5 µSv/h)
Courtesy Franck Peauger
Concrete block - RP

## Slide 38: Outline
  Accelerator ingredient
  Accelerator Environment: Superfluidity and Superconductivity
  Application to Cavity:
    Cavity model
    Cryomodules function
    SRF cavity fabrication
    Cavity package
    Cryomodules
  Application to Magnet: cryo-magnets at LHC
Notes: Zoom in ( previous talk on magnets and cavity)

## Slide 39: Cavities package to Cryomodules
RF cavities housed in cryomodules, which keep the SRF cavities working in a superconducting state, without losing energy to electrical resistance

## Slide 40: Spoke cryomodule
Thermal shield
T° -200°C
Supports
A cryomodule: what is it and what for?
Thermal conduction
RF electro magnetic wave (352 MHz)
Superconducting radiofrequency (SRF) cavity
T°-269°C
Thermal radiation
Room T°
Vacuum
Vacuum
1/ To provide a cryogenic environment to the cold mass (cavity) = cryostat:
- distributing the cryofluids to cool-down and maintain at cold T° (LHe, LN2)
- limiting the heat transfers
Vessel
Courtesy Patxi Duthill

## Slide 41: Spoke cryomodule
A cryomodule: what is it and what for?
Supports
Vacuum vessel
2/ To support the cavities and perform accurate alignment
- with respect to the beam axis
- with respect to other linac components (cryomodules, diagnostics, tunnel)
NB: alignment must be preserved during thermal and pressure cycles
Supports
Tunnel
Cryomodule
Diag

## Slide 42: Spoke cryomodule
A cryomodule: what is it and what for?
Vacuum vessel
3/ To offer magnetic shielding
- from the local magnetic sources
- from the earth magnetic shield
NB: the magnetic shield might be cooled (for better performances)
Magnetic shield

## Slide 43: Spoke cryomodule
A cryomodule: what is it and what for?
Vacuum vessel
4/ To provide all interfaces between the cavity and the tunnel:
- beam pipe
- RF
- cryogenic
- vacuum
- diagnostic (instrumentation)
- mechanical (support and alignment)

## Slide 44: The Spoke cryomodule prototype
Other components
 Gate valves
 Assembly tests
Smaller/less parts inside the clean room
Thermal optimization
 Cold warm transitions

## Slide 45: The Spoke cryomodule
Other components
    Supporting system :
    rods based solution
     possibility of adjusting the alignment under vacuum and cryogenic working conditions
     Optical monitoring system for alignment diag. inside the cold CM
    Thermal and thermo-mechanical optimization
    Rod made of two parts for easier cryostating
Inner rod
Outer rod
    Easier assembly (simpler tooling)
    Support rods fabricated
    Support tested

## Slide 46: The Spoke cryomodule prototype
Cryomodule thermal shield
    Material: Al6062
    Thickness: 2 mm
He 20 bars
(machine)
Sat N2
(Proto)
    Thermal shield fabricated
    Assembled and supported (rods)
    Instrum. and cool-down test

## Slide 47: The Spoke cryomodule prototype
Cavities magnetic shield
Tuner side ends
Cavity bellow side ends
External shield
Coupler shield
Internal shield
Cooling circuit
Shield support
Shrim
Material: Cryophy®
Actively cooled (better performances)
    Magnetic shields fabricated
    Assembly test performed
    To be tested within the cryomodule

## Slide 48: Outline
  Accelerator ingredient
  Accelerator Environment: Superfluidity and Superconductivity
  Application to Cavity:
    Cavity model
    SRF cavity fabrication
    Cryomodules function
    Cavity package
    Cryomodules
  Application to Magnet: cryo-magnets at LHC
Notes: Zoom in ( previous talk on magnets and cavity)

## Slide 49: Cavity package
Doorknob – Transition between
the coaxial power coupler and
the WR2300 rectangular waveguide
Double Spoke Cavity
Heat exchanger necessary to make
the transition from 300 K to 2 K
Integrating a mechanical system
to compensate efforts
RF Power Coupler

## Slide 50: Cavities tuning: Lorentz De-tuning
Because of the enormous gradients in superconducting cavities,
  the radiation pressure deforms the cavities
We expect over 400 Hz of detuning in the ESS cavities
  Unloaded cavity bandwidth = 0.07 Hz
  Loaded cavity bandwidth = 1 kHz
The mechanical time constant of the cavities is about 1 ms compared to the pulse length of 3 ms
  Static pre-detuning as done in SNS will not be sufficient
  Dynamic de-tuning compensation using piezo-electric tuners is a must!
  Or else pay for the extra RF power required
ESS and long pulse: 2.86 ms

## Slide 51: Cold Tuning System
2 piezo stacks
Stepper motor and planetary gearbox (1/100e) at cold and in vacuum
Slow tuner
Main purpose : Compensation of large frequency shifts with a low speed
Actuator used : Stepper motor
Fast tuner
Main purpose : Compensation of small frequency shifts with a high speed
Actuator used : Piezoelectric actuators
Type V ; 5-cell prototype
+/- 3 mm range on cavity
Elliptical CTS
Spoke CTS
&

## Slide 52: Cold Tuning System

## Slide 53: Fundamental Power Coupler
Antenna
Vacuum
Outer conductor
(LHe-cooled)
Doorknob
Inner conductor
(water-cooled)
Al2O3
ceramic disc
RF input
Short circuit
WR2300
Elliptical:
1.1 MW
Spoke:
335 kW